## Slide 2
LW-16-18

## Slide 3
Function of Waxes in
PVC Pipe Extrusion
Thomas C. Pedersen
Rheogistics LLC
Picayune, MS USA

## Slide 4: Rigid PVC Lubricants
Paraffin waxes have been used for more than 40 years to lubricate rigid PVC.

## Slide 5: Rigid PVC Lubricants
Paraffin Waxes
Calcium Stearate
Polyethylene Waxes
Montan Waxes – the earliest standard
  Hoechst Wax E & OP
  Esters of Montanic acid
Fatty Acid Esters
  Derived from natural oils and fats
Amide Waxes
  Ethylene bisstearamide wax

## Slide 6: Rigid PVC Lubricants
Prevent rigid PVC from degrading when heated and sheared.
Define rheology and control fusion.
Allow the compound to be adjusted to the process.
The keys to better rigid PVC products and processing.

## Slide 7: Rigid PVC
Most rigid PVC properties are affected in one way or another by the lubricant system.
Getting and keeping things right is a constant balancing act.

## Slide 8: Poly Vinyl Chloride
Rigid PVC has great properties
  Typical 7000+ psi tensile strength
  Excellent stiffness
  Excellent impact strength
  Very good weatherability
  Excellent cost performance

## Slide 9: PVC Resin

## Slide 10: PVC Compound

## Slide 11: Processing Rigid PVC
Rigid PVC products are formed by heating and compressing PVC compounds into desired shapes.
The compound is compressed from a bulk density of approximately 0.50 gm/ml to a product density of approximately 1.40 gm/ml
PVC is heated to ca. 400°F by mechanical shear and heat transfer.
During processing, PVC is exposed to pressures of 2000 to 4000 psi.

## Slide 12: PVC Processing
The 0.7-1 micron PVC primary particles are thought to be the primary flow units during rigid PVC processing

## Slide 13: Rigid PVC Fusion in Extrusion

## Slide 14: Effects of Fusion Levels on Physical Properties
Tensile Properties
  Increase with increasing fusion
Impact Properties
  Peak at an intermediate level of fusion

## Slide 15: Extruder Energy Balance

## Slide 16: Typical Rigid PVC Pipe Formulation
PVC Resin
Tin Stabilizer
Lubricants
Calcium Carbonate
Pigments

## Slide 17: Plastic Pipe Institute’s TR-2 PVC Pipe Formulation
Ingredient Usage Level
PVC Resin 100.0 parts
Tin Stabilizer 0.30 – 1.00 phr
Paraffin Wax 0.60 – 1.50 phr
Polyethylene Wax 0.00 – 0.30 phr
Calcium Stearate 0.40 – 1.50 phr
Calcium Carbonate 0.00 – 5.00 phr
Titanium Dioxide 0.50 – 3.00 phr
Process Aid 0.00 – 2.00 phr

## Slide 18: Typical Rigid PVC Lubricant System
Paraffinic Hydrocarbon Wax
    Refined from crude or synthetic based on ethylene or methane
    Typical C32H66
Calcium Stearate
    Calcium salt of acid from natural fats and oils
    Ca(C18H35O2)2
Oxidized PE Wax
    Ethylene based
    C100+H200+O?

## Slide 19: Plastic Pipe Institute TR-2 Part A.3 Paraffinic Hydrocarbon Wax Specification

## Slide 21
Formulating waxes to meet
the PPI specification will result in rigid PVC formulations with different processing characteristics and physical properties.

## Slide 22
If formulating waxes for rigid PVC, keep in mind what Mark Twain said:
“It ain't what you don't know that gets you into trouble. It's what you know for sure that just ain't so.”

## Slide 23
The only reliable predictor of hydrocarbon wax performance in rigid PVC:
The size, shape, and numbers of wax molecules.

## Slide 24: Typical Rigid PVC Lubricant System
Paraffinic Hydrocarbon Wax
    Refined from crude or synthetic based on ethylene or methane
    Typical C32H66
Calcium Stearate
    Calcium salt of acid from natural fats and oils
    Ca(C18H35O2)2
Oxidized PE Wax
    Ethylene based
    C100+H200+O?

## Slide 25: Rigid PVC Lubricants Product Options
Individual Ingredients
Combinations of multiple lubricants (Paraffin, oPE, etc.)
Total systems include paraffin, oPE, and calcium stearate
Dust free, free flowing, fully melting calcium stearate

## Slide 26: Fusion Characterization in the Lab
Torque Rheometer
  Fixed volume heated chamber
  Work imparted into PVC compound by mixing blades
  Measure torque required to turn the blades and melt temperature

## Slide 27: Trial PVC Compound
PVC Resin 100 parts
Stabilizer 0.50 phr
Wax 1.30 phr
Calcium Stearate 0.65 phr
Oxidized PE Wax 0.15 phr
Calcium Carbonate 5.00 phr
Titanium Dioxide 0.50 phr

## Slide 28: Paraffin Waxes
Paraffin waxes are mixtures of branched and straight chain molecules
  Normal Straight Chain Content
  CH3CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH3
  Branched or “Non-normal” Content
  CH3
  CH3CH2CH2CH2CH2CH2CH2CH1CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH1CH2CH2CH2CH2CH2CH2CH2CH3
  CH2
  CH2
  CH3
  Over 1,000,000 different C32+ H66+ molecular structures are possible.

## Slide 29: Effect of Wax Molecule Size on Rheology
Carbon Number | Fusion Time | Fusion Torque | Equil. Temp
26 | 166 sec | 21.3 Nm | >195°C.
32 | 352 sec | 15.2 Nm | 188°C.
40 | 2,120 sec | 10.1 Nm | 188°C.
100+ (PE Wax) | 182 sec | 18.9 Nm | >195°C.
C26 more soluble in rigid PVC. C40+ insoluble in rigid PVC.

## Slide 32: Lubricants are Mechanical Stabilizers
Lubricants prevent rigid PVC from degrading when heated and sheared.
Lubricants are often adjusted to eliminate shear burning issues.
In the USA, many rigid PVC formulations run very low levels of tin stabilizer and rely on lubrication for adequate stability.

## Slide 33: Mechanical Stabilization of Rigid PVC
Recent Rheogistics Study
Could rigid PVC be processed without a conventional heat stabilizer? What happens when heat stabilizer is reduced or eliminated?

## Slide 34: Plastic Pipe Institute’s TR-2 PVC Pipe Formulation
Ingredient Usage Level
PVC Resin 100.0 parts
Tin Stabilizer 0.30 – 1.00 phr
Paraffin Wax 0.60 – 1.50 phr
Polyethylene Wax 0.00 – 0.30 phr
Calcium Stearate 0.40 – 1.50 phr
Calcium Carbonate 0.00 – 5.00 phr
Titanium Dioxide 0.50 – 3.00 phr
Process Aid 0.00 – 2.00 phr

## Slide 35: PPI PVC Pipe Range Composition Lubrication Limits
Minimum
Allowable
Lubricants,
0.60/0.00/0.40
Maximum Allowable
Lubricants,
1.50/0.30/1.50

## Slide 36: Mechanical Stabilization of Rigid PVC
Pipe Grade PVC Resin 100.0 parts
RX-165 Paraffin Lubricant 1.30 phr
RX-215 Oxidized Polyethylene 0.15 phr
Calcium Stearate 0.65 phr
Calcium Carbonate 5.00 phr
Titanium Dioxide 1.00 phr
19% Methyl Tin Stabilizer 0.50 phr, 0.25 phr, 0.125 phr,
0.0625 phr and zero
Processed on a Brabender Torque Rheometer for one hour (65 gram charge,
60 rpm, 175° set point, no cooling)

## Slide 37: Rigid PVC – Higher Stabilizer
0.50 phr
0.25 phr

## Slide 38: Rigid PVC – Lower Stabilizer
0.125 phr
0.0625 phr

## Slide 39: Rigid PVC – Lubricants Only
ZERO Tin

## Slide 40: Reducing Tin Stabilizer
Shifts rheology
Fusion time and torques remain remarkably similar
Post fusion torque decrease occurs quicker
Longer term melt torque and temperature remain remarkably stable
Melt exhibits more “chatter”

## Slide 41: Mechanical Stabilization of Rigid PVC Color Development

## Slide 42: Mechanical Stabilization of Rigid PVC Color Development
As the level of tin stabilizer is reduced, color develops more quickly.
When tin stabilizer is not present, early pinking becomes an issue.

## Slide 43: Conclusions
The PVC Industry is a large application for paraffin and hydrocarbon waxes.
Simple alkanes (paraffin waxes) are very versatile and effective primary lubricants for rigid PVC.

## Slide 44: Conclusions
Waxes with carbon numbers of C30 to C34 work best as primary PVC lubricants in North America’s tin stabilized formulations.
In addition to their role in managing rheology, lubricants serve as mechanical stabilizers.
Rigid PVC free of conventional heat stabilizers may be processed under certain conditions.

## Slide 45: Conclusions
The lubricant system is adjusted to tune the formulation to the heating and shearing characteristics of the customer’s processing equipment.
Changes in any material or any piece of equipment in a customer’s plant results in the need for a lubricant adjustment.

## Slide 46: Conclusions
Understanding and managing lubricant performance in rigid PVC is very complex.
The PVC industry requires in-depth technical support and service.

## Slide 47: Conclusions
The paraffin wax, calcium stearate, and oxidized polyethylene wax long used in the USA is an excellent starting point for alternate stabilization systems.

## Slide 48: References
T. C. Pedersen, “Process and Material Considerations in the Industrial Application of Lubricants in Rigid PVC Extrusion”, Journal of Vinyl Technology, 6, 104 (1984)
J. W. Summers, “Lubrication Mechanism in Poly (Vinyl Chloride) Compounds: Understanding the Three Distinct Roles of Lubricants” Antec 2006, Society of Plastics Engineers.
P. Benjamin, “The Influence of Processing on the Properties of PVC Pipe”, International Conference on PVC Processing, 6 & 7 April 1978, The Plastics and Rubber Institute.
TR-2, Plastic Pipe Institute PVC Pipe Range Composition, List of Qualified Ingredients, 19 March 2013, Plastics Pipe Institute, Irving, TX USA

## Slide 49
Thank You!
Technology for Better Rigid PVC