## Slide 1
Lubrication and Mechanical Stabilization
of Rigid PVC Formulations
Thomas C. Pedersen
Rheogistics LLC
Picayune, MS USA

## Slide 2: Typical Rigid PVC Pipe Formulation
PVC Resin
Tin Stabilizer
Lubricants
Calcium Carbonate
Pigments

## Slide 3: Widely Used Rigid PVC Lubricants
Paraffin Waxes
Calcium Stearate
Polyethylene Waxes
Montan Waxes – the earliest standard
  Hoechst Wax E & OP
  Esters of Montanic acid
Fatty Acid Esters
  Derived from natural oils and fats
Amide Waxes
  Ethylene bisstearamide wax

## Slide 4: Rigid PVC Lubricants
Prevent rigid PVC from degrading when heated and sheared.
Define rheology and control fusion.
Allow the compound to be adjusted to the process.
The keys to better rigid PVC products and processing.

## Slide 5: Rigid PVC Lubricants
Paraffin waxes have been used for more than 40 years to lubricate rigid PVC.
Large volume rigid PVC applications using paraffin waxes as the primary lubricant include:
                PVC Pipe
                Vinyl Siding
                Vinyl Windows
                PVC Fencing
                PVC Boards

## Slide 6: Typical Rigid PVC Lubricant System
Paraffinic Hydrocarbon Wax
    Refined from crude or synthetic based on ethylene or methane
    Typical C32H66
Calcium Stearate
    Calcium salt of acid from natural fats and oils
    Ca(C18H35O2)2
Oxidized PE Wax
    Ethylene based
    C100+H200+O?

## Slide 7: Rigid PVC Lubricants Product Options
Individual Ingredients
Combinations of multiple lubricants (Paraffin, oPE, etc.)
Total systems include paraffin, oPE, and calcium stearate
Dust free, free flowing, fully melting calcium stearate

## Slide 8: Paraffin Waxes
Paraffin waxes are mixtures of branched and straight chain molecules
  Normal Straight Chain Content
  CH3CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH3
  Branched or “Non-normal” Content
  CH3
  CH3CH2CH2CH2CH2CH2CH2CH1CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH1CH2CH2CH2CH2CH2CH2CH2CH3
  CH2
  CH2
  CH3
  Over 1,000,000 different C32+ H66+ molecular structures are possible.

## Slide 9: Effect of Wax Molecule Size on Rheology
Carbon Number | Fusion Time | Fusion Torque | Equil. Temp
26 | 166 sec | 21.3 Nm | >195°C.
32 | 352 sec | 15.2 Nm | 188°C.
40 | 2,120 sec | 10.1 Nm | 188°C.
100+ (PE Wax) | 182 sec | 18.9 Nm | >195°C.
C26 more soluble in rigid PVC. C40+ insoluble in rigid PVC.

## Slide 10: Lubricants are Mechanical Stabilizers
Lubricants prevent rigid PVC from degrading when heated and sheared.
Lubricants are often adjusted to eliminate shear burning issues.
In the USA, many rigid PVC formulations run very low levels of tin stabilizer and rely on lubrication for adequate stability.

## Slide 11: Mechanical Stabilization of Rigid PVC
Recent Rheogistics Study
Could rigid PVC be processed without a conventional heat stabilizer? What happens when heat stabilizer is reduced and eliminated?

## Slide 12: Mechanical Stabilization of Rigid PVC
Pipe Grade PVC Resin 100.0 parts
RX-165 Paraffin Lubricant 1.30 phr
RX-215 Oxidized Polyethylene 0.15 phr
Calcium Stearate 0.65 phr
Calcium Carbonate 5.00 phr
Titanium Dioxide 1.00 phr
19% Methyl Tin Stabilizer 0.50 phr, 0.25 phr, 0.125 phr,
0.0625 phr and zero
Processed on a Brabender Torque Rheometer for one hour (65 gram charge,
60 rpm, 175° set point, no cooling)

## Slide 13: Rigid PVC – Higher Stabilizer
0.50 phr
0.25 phr

## Slide 14: Rigid PVC – Lower Stabilizer
0.125 phr
0.0625 phr

## Slide 15: Rigid PVC – Lubricants Only
ZERO Tin

## Slide 16: Reducing Tin Stabilizer
Shifts rheology
Fusion time and torques remain remarkably similar
Post fusion torque decrease occurs quicker
Longer term melt torque and temperature remain remarkably stable
Melt exhibits more “chatter”

## Slide 17: Mechanical Stabilization of Rigid PVC Color Development

## Slide 18: Mechanical Stabilization of Rigid PVC Color Development
As the level of tin stabilizer is reduced, color develops more quickly.
When tin stabilizer is not present, early pinking becomes an issue.

## Slide 19: Post Fusion Torque
Why does the melt torque substantially decrease after fusion even as the melt temperature remains relatively stable?
“There’s something happening here, what it is ain’t exactly clear……”

## Slide 20: PPI PVC Pipe Range Composition Lubrication Limits
Minimum
Allowable
Lubricants,
0.60/0.00/0.40
Maximum Allowable
Lubricants,
1.50/0.30/1.50

## Slide 21: Ideal Post Fusion Torque Example RX-7 Calcium Stearate Free Formulation
Tin Stabilized
Mechanical Only

## Slide 22: Conclusions
In addition to their role in managing rheology, lubricants serve as mechanical stabilizers.
Rigid PVC free of conventional heat stabilizers may be processed under certain conditions.
Simple alkanes (paraffin waxes) are very versatile and effective primary lubricants for rigid PVC.

## Slide 23: Conclusions
The post fusion torque decrease often observed in rigid PVC formulations is related to a complex phenomena involving calcium stearate.
The paraffin wax, calcium stearate, and oxidized polyethylene wax long used in the USA is an excellent starting point for alternate stabilization systems.

## Slide 24
Thank You!
Technology for Better Rigid PVC