## Slide 1
Mechanical Stabilization of
Rigid PVC Compositions

## Slide 2: Mechanical Stabilization of Rigid PVC Compositions
Thomas C. Pedersen & Robert R. Kwapisz, Jr.
Rheogistics LLC
Picayune, MS USA

## Slide 3: PPI TR-2 PVC Pipe Formulation
Ingredient Usage Leve
PVC Resin 100.0 parts
Tin Stabilizer 0.30 – 1.00 phr
Paraffin Wax 0.60 – 1.50 phr
Polyethylene Wax 0.00 – 0.30 phr
Calcium Stearate 0.40 – 1.50 phr
Calcium Carbonate 0.00 – 5.00 phr
Titanium Dioxide 0.50 – 3.00 phr
Process Aid 0.00 – 2.00 phr

## Slide 4: Rigid PVC Lubricants
Define rheology and control fusion.
Allow the compound to be adjusted to the process.
The keys to better rigid PVC products and processing
Prevent rigid PVC from degrading when heated and sheared

## Slide 5: Rigid PVC Lubricants
Paraffin waxes have been used for more than 40 years to lubricate rigid PVC.
Large volume rigid PVC applications using paraffin waxes as the primary lubricant include:
                PVC Pipe
                Vinyl Siding
                Vinyl Windows
                PVC Fencing
                PVC Boards

## Slide 6: Typical Rigid PVC Lubricant System
Paraffinic Hydrocarbon Wax
    Refined from crude or synthetic based on ethylene or methane
    Typical C32H66
Calcium Stearate
    Calcium salt of acid from natural fats and oils
    Ca(C18H35O2)2
Oxidized PE Wax
    Ethylene based
    C100+H200+O?

## Slide 7: Paraffin Waxes
Paraffin waxes are mixtures of branched and straight chain molecules
  Normal Straight Chain Content
  CH3CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH3
  Branched or “Non-normal” Content
  CH3
  CH3CH2CH2CH2CH2CH2CH2CH1CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH2CH1CH2CH2CH2CH2CH2CH2CH2CH3
  CH2
  CH2
  CH3
  Over 1,000,000 different C32+ H66+ molecular structures are possible.

## Slide 8: Effect of Molecular Size on Rheology
Carbon Number | Fusion Time | Fusion Torque | Equil. Temp
26 | 166 sec | 31.2 Nm | >195°C.
32 | 352 sec | 15.2 Nm | 188°C.
40 | 2,120 sec | 10.2 Nm | 188°C.
100+ | 182 sec | 18.9 Nm | >195°C.
C26 more soluble in rigid PVC. C40+ less soluble in rigid PVC.

## Slide 9: Rigid PVC Lubricants
Lubricants prevent rigid PVC from degrading when heated and sheared.
Lubricants are often adjusted to eliminate shear burning issues.
In the USA, many rigid PVC formulations run very low levels of tin stabilizer and rely on lubrication for adequate stability.

## Slide 10: Recent Rheogistics Study
What happens when heat stabilizer is reduced and eliminated?
Could rigid PVC be processed without a conventional heat stabilizer?
Are lubricants mechanical stabilizers?

## Slide 11: Mechanical Stabilization of Rigid PVC
Pipe Grade PVC Resin 100.0 parts
RX-165 Paraffin Lubricant 1.30 phr
RX-215 Oxidized Polyethylene 0.15 phr
Calcium Stearate 0.65 phr
Calcium Carbonate 5.00 phr
Titanium Dioxide 1.00 phr
19% Methyl Tin Stabilizer 0.50 phr, 0.25 phr, 0.125 phr,
0.0625 phr and zero
Processed on a Brabender Torque Rheometer for one hour (65 gram charge,
60 rpm, 175° set point, no cooling)

## Slide 12: Rigid PVC – Higher Stabilizer
0.50 phr
0.25 phr

## Slide 13: Rigid PVC – Lower Stabilizer
0.125 phr
0.0625 phr

## Slide 14: Rigid PVC – Lubricants Only
Zero Tin

## Slide 15: Reducing Tin Stabilizer
Shifts rheology
Fusion time and torques remain remarkably similar
Post fusion torque decrease occurs quicker
Longer term melt torque and temperature remain remarkably stable
Melt exhibits more “chatter”

## Slide 16: Mechanical Stabilization of Rigid PVC Color Development

## Slide 17: Mechanical Stabilization of Rigid PVC Color Development
As the level of tin stabilizer is reduced, color develops more quickly.
When tin stabilizer is not present, early pinking becomes an issue.

## Slide 18: Conclusions
In addition to their role in managing rheology, lubricants serve as mechanical stabilizers.
Rigid PVC free of conventional heat stabilizers may be processed under certain conditions.
Simple alkanes (paraffin waxes) are very versatile and effective primary lubricants for rigid PVC.

## Slide 19: Conclusions
The paraffin wax, calcium stearate, and oxidized polyethylene wax long used in the USA is an excellent starting point for alternate stabilization systems.

## Slide 20: Thank You!